## Slide 1: Accurate viscoelastic large deformation analysis using F-bar aided edge-based smoothed finite element method for 4-node tetrahedral meshes (F-barES-FEM-T4)
Yuki ONISHI, Ryoya IIDA, Kenji AMAYA Tokyo Institute of Technology, Japan

## Slide 2: Motivation
What we want to do:
Solve hyper large deformation analyses accurately and stably.
Treat complex geometries with tetrahedral meshes.
Consider nearly incompressible materials .
Support contact problems.
Handle auto re-meshing.
Rubber
Plastic/Glass
Metal

## Slide 3: Issues
Conventional tetrahedral (T4/T10) FE formulations still have issues in accuracy or stability especially in nearly incompressible cases.
2nd or higher order elements: ✗ Volumetric locking. Accuracy loss in large strain due to intermediate nodes.
Enhanced assumed strain method (EAS): ✗ Spurious low-energy modes.
B-bar method, F-bar method, Selective reduced integration: ✗ Not applicable to tetrahedral element directly.
F-bar-Patch method: ✗ Difficulty in building good-quality patches.
u/p mixed (hybrid) method: (e.g., ABAQUS/Standard C3D4H and C3D10MH) ✗ Pressure checkerboarding, Early convergence failure etc..

## Slide 4: Issues (cont.)
E.g.) Compression of neo-Hookean hyperelastic body with
1st order hybrid T4 (C3D4H)
 No volumetric locking
✗ Pressure checkerboarding
✗ Shear & corner locking
2nd order modified hybrid T10 (C3D10MH)
 No shear/volumetric locking ✗ Early convergence failure
✗ Low interpolation accuracy
# of Nodes is almost the same.
Pressure
Pressure

## Slide 5: A Recent Solution
A new idea of FE formulation called “Smoothed Finite Element Method (S-FEM)” was recently proposed and is in researching today widely.
Our group has proposed a latest S-FEM named “F-barES-FEM-T4” (detailed later):
  No intermediate node & No additional DOF, (i.e., Purely displacement-based 4-node tetrahedral (T4) element),
  Free from shear, volumetric and corner locking,
  No pressure checkerboarding,
  Long lasting in large deformation.

## Slide 6: A Recent Solution (cont.)
e.g.1) Compression of hyperelastic body with
F-barES-FEM-T4 (One of the latest S-FEM)  No shear/volumetric locking
 No corner locking  No pressure checkerboarding
Same mesh as C3D4H case.
Pressure

## Slide 7: A Recent Solution (cont.)
e.g.2) Shear of elastoplastic body with soft hardening coeff.
1st order hybrid T4 (C3D4H)
 No volumetric locking
✗ Shear locking
✗ Pressure checkerboarding
F-barES-FEM-T4  No volumetric locking
 No shear locking  No pressure checkerboarding
Pressure
We have evaluated F-barES-FEM-T4 in elastic and elastoplastic cases but NOT in viscoelastic cases yet.

## Slide 8: Objective
To apply and demonstrate the latest S-FEM called F-barES-FEM-T4 to viscoelastic large deformation problems.
Table of Body Contents
Introduction of F-barES-FEM-T4’s formulation
Demonstration of F-barES-FEM-T4 in viscoelastic problems
Summary

## Slide 9
Introduction of F-barES-FEM-T4’s formulation

## Slide 10: 1. Brief of Edge-based S-FEM (ES-FEM)
Calculate at each element as usual.
Distribute to the connecting edges with area weight and build .
Calculate etc. in each edge smoothing domain.
As if putting an integration point on each edge center
✗ Volumetric locking ✗ Pressure checkerboarding
No shear locking
No spurious modes

## Slide 11: 2. Brief of Node-based S-FEM (NS-FEM)
Calculate at each element as usual.
Distribute to the connecting nodes with area weight and build .
Calculate etc. in each node smoothing domain.
As if putting an integration point on each node
✗ Spurious low-energy mode
Less pressure checkerboarding
No shear locking
No volumetric locking

## Slide 12: 3. Brief of F-bar Method
Algorithm
Calculate deformation gradient at the element center, and then make the relative volume change .
Calculate deformation gradient at each gauss point as usual, and then make ) .
Modify at each gauss point to obtain as
.
Use to calculate the stress , nodal force etc..
For quadrilateral (Q4) or hexahedral (H8) elements
A kind of low-pass filter for
✗ Shear locking
Less pressure checkerboarding
No volumetric locking
No spurious modes

## Slide 13: Outline of F-barES-FEM
Concept: combine ES-FEM and NS-FEM using F-bar method
Outline
is given by ES-FEM.
is given by cyclically (c times) applied NS-FEM.
is calculated in the manner of F-bar method:
.

## Slide 14: How to Treat Viscoelastic Model
Stress
Time advance of viscous strain
Equation to solve
Prony coeff
Viscous strain
Hencky (Logarithmic) strain
Bulk modulus
Instantaneous shear modulus
Rigid rotation in an increment
Viscous strain increment
Same as static problems due to the absence of inertia.
Viscosity only in deviatoric stress.
The target constitutive model to treat is the Hencky’s viscoelastic model based on the generalized Maxwell model.
The most standard one.

## Slide 15
Demonstration of F-barES-FEM-T4 in viscoelastic problems

## Slide 16: Tensile Suspension of Viscoelastic Block
Outline
block subjected to 100% stretch in 10 s, and hold the enforced displacement for 1000 s under the gravity.
Hencky’s viscoelastic body based on the generalized Maxwell model with 1 maxwell element & 1 long-term spring.
  Poisson’s ratio: , and .
  Relaxation time: .
Compare the results of F-barES-FEM-T4(2), ABAQUS C3D4, C3D4H, and C3D8.
1405 nodes, 6183 elements.

## Slide 17: Tensile Suspension of Viscoelastic Block
Animation of Mises Stress (F-barES-FEM-T4(2))
Stress relaxation progresses after stretch.

## Slide 18: Tensile Suspension of Viscoelastic Block
Pressure at the end of stretch (common contour range)
ABAQUS C3D4
ABAQUS C3D8
ABAQUS C3D4H
F-barES-FEM-T4(2)
Checkerboarding
No Checkerboarding!!

## Slide 19: Tensile Suspension of Viscoelastic Block
Pressure at the final state (common contour range)
ABAQUS C3D4
ABAQUS C3D8
ABAQUS C3D4H
F-barES-FEM-T4(2)
Severe
Checkerboarding
Small Deflection
No Checkerboarding!!

## Slide 20: Tensile Suspension of Viscoelastic Block
Time histories of at the center of bottom face
ABAQUS’s T4 elements cannot avoid shear locking, whereas F-barES-FEM-T4 has good accuracy as H8-SRI element.
ABAQUS
C3D4 and
C3D4H have shear locking.

## Slide 21: Body Forced Stretch of Viscoelastic Bunny
Outline
A Stanford bunny subjected to stretch under the body force.
Same viscoelastic properties:
Hexahedral mesh is difficult to build.
Compare the results of F-barES-FEM-T4(2) and ABAQUS C3D4H.
Fixed
Body Force (Opposite Gravity)
24136 nodes, 126231 elements.

## Slide 22: Body Forced Stretch of Viscoelastic Bunny
Animation of Mises stress (F-bar ES-FEM -T4(2))
Smooth Mises stress distribution is obtained.
Necking occurred.

## Slide 23: Body Forced Stretch of Viscoelastic Bunny
ABAQUS C3D4H
Mises stress at the final state
Slightly small deformation due to shear locking.
F-bar ES-FEM -T4(2)
Similar Mises stress distribution.

## Slide 24: Body Forced Stretch of Viscoelastic Bunny
ABAQUS C3D4H
F-bar ES-FEM -T4(2)
Severe pressure checkerboarding.
Pressure at the final state
Smooth pressure distribution.

## Slide 25
Summary

## Slide 26: Benefits and Drawbacks of F-barES-FEM-T4
Benefits
  Locking-free with 1st order tetra meshes.
  No difficulty in severe strain or contact analysis.
  No increase in DOF.
  Purely displacement-based formulation.
  Long lasting.
  Less pressure checkerboarding.
Drawbacks
✗ The more cyclic smoothing necessitates the more CPU time due to the wider bandwidth.
More stable & accurate than other T4 elements!!!
Slower than other T4 elements…

## Slide 27: Take-Home Messages
F-barES-FEM-T4 is the current best T4 FE formulation for the large deformation with near incompressibility:
  Hyperelastic materials,
  Elastoplastic materials, and
  Viscoelastic materials.
Thank you for your kind attention!