## Slide 1: Numerical modeling method to reproduce UV imprint process using thermo-viscoelastic constitutive law
Ryunosuke YAMASHITA, Yuki ONISHI, Kenji AMAYA
Tokyo Institute of Technology, Japan

## Slide 2: Background
UV imprinting is a low cost and high throughput production method.
It has been adopted to the production of various optical devices requiring high surface accuracy such as micro mirror array.
PDMS Mold
UV Resin
Mold
Observer
Parity Mirror ®
Aerial image
Light source
UV Exposure & Demolding
UV Resin
Example of optical product produced by
micro imprint. (Parity Innovations Co., Ltd.)

## Slide 3: Issues
In the curing process, volume shrinkage of UV resin arises and may cause unintended surface curvature when a soft mold such as PDMS is used.
There is no numerical modeling method to reproduce this type of error in UV imprint, although there are a few conventional methods for thermal imprint.
UV Resin
Soft Mold
UV Resin
Soft Mold
Shrink
UV
Exposure
Demolding
Y. Onishi et al. Jpn. J. Appl. Phys. 47 5145 (2008)
UV Resin
✘
Unintended Surface Curvature

## Slide 4: Brief of Conventional Method for Thermal Imprint Simulation
Thermo-viscoelastic constitutive model
  Thermal contraction is described with thermal expansion coefficient.
  Shear behavior is described with the time- temperature superposition principle and Prony series for the generalized Maxwell model.
  Volumetric behavior is assumed to be independent of strain rate and temperature.
Numerical simulation with the finite element method (FEM)
Ginf
Gn
1
n
G1
Our idea：
Similar numerical approach could be used for UV imprint simulation.

## Slide 5: Objective
Propose a numerical method for UV curing process simulation.
Utilize the process simulation for mold shape optimization.

## Slide 6: Methods

## Slide 7: Overview of Our Method
Considering the analogy of thermal and UV imprint,
Our approach uses thermo-viscoelastic material constitutive model and replaces phenomena on UV resin as follows.
    UV reaction progress Cooling (temperature drop)
    UV shrink Cooling contraction
    UV curing Cooling solidification
The model parameters are identified through rheology measurement experiments.
Numerical UV process simulation is realized as the result.
Becomes similar to thermal imprint simulation

## Slide 8: Experimental Conditions
Rotational oscillatory rheometer (Anton Paar MCR301) is used.
The measurement object is an UV resin from Daicel Co..
Room temperature is 25℃ (const.).
UV exposure condition is constant (30 s exposure in a constant intensity).
The oscillation frequency is varied from 0.1 to 10 Hz.
The gap between the cylinder rod and the glass plate changes over time due to UV shrink.
Long time measurement is conducted to consider the dark curing.
Cylinder
Rod
Glass Plate
UV Resin
UV Light
Small Rotational Oscillation
Follow
Gap
Change
Gap
0 30 time (s)
Intensity

## Slide 9: Relative Gap Change (Experimental Result)
Time History of Relative Gap Change
Note: the time history of the relative gap change is always the same in all cases (∵ UV exposure condition is constant).
UV shrink progresses with time, but the shrink speed gradually decreases.

## Slide 10: Relative Gap Change (Model Parameter Identification)
UV shrink is modeled as thermal (cooling) contraction.
For the UV reaction progress measure, the time history of temperature is given as . (Note that is not a real physical quantity but just a virtual value.)
The time history of relative gap change is converted into the temperature-dependent coefficient of thermal expansion.
Temperature-Dependent Coefficient of Thermal Expansion
Note: is negative because it represents the volume change compared to the initial volume.

## Slide 11: Viscoelasticity (Experimental Result)
Time History of Storage / Loss Shear Modulus ()
Depending on the frequency, the time histories of and are different (harder at higher frequencies).
At any frequency, UV resin monotonically hardens with time.

## Slide 12: Viscoelasticity (Model Parameter Identification 1/3)
UV resin is modeled as viscoelastic material based on the time-temperature superposition principle and Prony series for the generalized Maxwell model.
A certain temperature is set as a reference temperature (e.g., ).
Pick s and s at different temperatures and identify each time shift.
Time-Shifted Storage Shear Modulus at (Master Curve)
P. 12
In practice, is also taken into consideration to determine the time shifts.
Shift for
Shift for
Shift for
Shift for
Shift for
Measurement at

## Slide 13: Viscoelasticity (Model Parameter Identification 2/3)
A temperature-dependent shift factor (i.e., time-temperature superposition) is obtained by fitting the time-shifts at various temperatures.
Temperature- Dependent Shift Factor

## Slide 14: Viscoelasticity (Model Parameter Identification 3/3)
Find the Prony series coeffs by fitting the master curve at the reference temp.
Storage / Loss Shear Modulus at Reference Temp. Expressed by Prony Series
From the above, the constitutive model of thermo-viscoelasticity to simulate UV shrink and curing were identified.

## Slide 15: Result & Discussion

## Slide 16: UV Curing Process Simulation (Outline)
Commercial finite element code, ABAQUS, is adopted.
Target pattern is a micro mirror array.
The mold pattern is periodic and thus only one mirror is taken into account with periodic boundary conditions.
Mold cavity is filled with UV resin at the initial state.
Temperature is given as .
UV exposure condition is exactly the same as that of the rheology measurement experiments. (30 s exposure in a constant intensity).
Demolding is conducted 70 s after the end of UV exposure.
Mirror curvature is evaluated enough after the demolding (6000 s).
Mirror Surface
PDMS Mold
UV Resin
3D View
320 m
320 m

## Slide 17: UV Curing Process Simulation (Outline)
Commercial finite element code, ABAQUS, is adopted.
Target pattern is a micro mirror array.
The mold pattern is periodic and thus only one mirror is taken into account with periodic boundary conditions.
Mold cavity is filled with UV resin at the initial state.
Temperature is given as .
UV exposure condition is exactly the same as that of the rheology measurement experiments. (30 s exposure in a constant intensity).
Demolding is conducted 70 s after the end of UV exposure.
Mirror curvature is evaluated enough after the demolding (6000 s).
Demolding
No-slip &
No-separation
Contact
Periodic Boundary Condition
UV Resin
PDMS Mold
2D View

## Slide 18: UV Curing Process Simulation (Simulation Result)
Displacement Dist. in X Direction
Deformation Scale Factor: 30 x 30 x 1 in XYZ
Sectional view (cut on plane)
Surface curvature due to the mold deformation is observed.
3D view
Flow of UV resin due to the UV shrink is observed.

## Slide 19: UV Curing Process Simulation (Validation)
Curvature Depth Dist. on Mirror Surface
Simulation Result (For ease of comparison, the contour color scheme uses “reversed rainbow”.)
Experimental Result (Measured with scanning probe microscope)
✔ Simulation result agreed with the experimental measurement data qualitatively.
The maximum curvature depth is about 1 m located at lower center of the surface.

## Slide 20: Mold Shape Optimization (Outline)
Unoptimized Mold Shape
UV Exposure
✘ Curvature!
Before Mold Optimization
After Mold
Optimization
Optimized Mold Shape
✔ Lesser Curvature!
UV Exposure

## Slide 21: Mold Shape Optimization (Simulation Result)
Curvature Depth Dist. on Mirror Surface
Simulation Result with Unoptimized Mold ✘ Maximum curvature depth: 1 µm
Simulation Result with Optimized Mold ✔ Maximum curvature depth: 0.01 µm
The optimized mold greatly suppressed the curvature and achieved a super-flat mirror surface!

## Slide 22: Summary

## Slide 23: Summary
A numerical modeling method for UV shrink & curing simulation using thermo-viscoelastic model was proposed.
The model parameters were identified through the rheology measurement experiments.
A process simulation for micro mirror array using PDMS mold validated the qualitative accuracy on mirror surface curvature.
A demonstration of mold shape optimization successfully suggested an optimal mold shape to achieve a flat mirror surface.
Quantitative validation and application to other patterns (such as lens arrays) are our future work.

## Slide 24: Acknowledgement
This is a joint work with Daicel Co. and Osaka Prefecture Univ. (Prof. Hirai’s group).
Another joint work is scheduled for oral presentation tomorrow:
  Yoshihiko Hirai et al., “3-Dimensional mold profile correction for resin shrinkage in micro-nano molding process”
  Sep. 26 (Wed.), 16:25 -16:40, Auditorium 11 (06-11: Metrology)
Thank you for your kind attention.

## Slide 25: Appendix

## Slide 26: Limitation of Our Method
UV exposure condition to simulate must be exactly the same as that on the rheology measurement experiments.
The pattern size must be large enough to apply continuum approximation.

## Slide 27: Validation of Material Constitutive Model
Outline
Finite element analyses using the identified thermo-viscoelastic properties to reproduce the rheometer measurement data is conducted.
For simplicity, time evolution analysis that gives shear vibration to one hexahedral element is performed.
Defined thermo-viscoelastic properties are:
  Temperature-dependent coefficient of thermal expansion,
  Temperature-dependent shift factor,
  Prony series at reference temperature,
  Instantaneous Young’s modulus and Poisson’s ratio
Field condition of temperature is given.
Boundary conditions are:
  Perfect constraint on the lower surface
  Small oscillatory disp. In shear on the upper surface.
Small shear oscillation

## Slide 28: Validation of Material Constitutive Model
Time History of Relative Gap Change
The relative gap change is accurately simulated.

## Slide 29: Validation of Material Constitutive Model
Time History of Storage / Loss Shear Modulus
The storage shear modulus is accurately simulated. On the other hand, minor problem remains in the accuracy of the loss shear modulus because .

## Slide 30: Outline of UV Process Simulation
Step 1: Stationary (1 sec.)
  Static analysis
  Start no-slip & no-separation contact
Step 2: UV curing (100 sec.)
  Quasi-static analysis
  Lower UV resin temperature:
Step 3: Demolding & Dark curing (6000 sec.)
  Quasi-static analysis
  Remove no-slip & no-separation contact
  Lift mold upward
  Continue lowering UV resin temperature:
Displacement 400µm
No-slip &
No-separation
contact
Periodic boundary condition
UV Resin
℃
PDMS Mold
ABAQUS/Standard C3D8 is used for FE analysis.

## Slide 31: Search Flow of Optimized Mold Shape
Forced
Displacement
Initial mold shape
Modify mold shape
①
UV process simulation
Get curvature data
Cost function： Squared sum of curvature depth
Optimization method: Quasi-Newton method
③ Mold shape update
②
Modify mold shape according to the curvature
This optimization loop continues until the curvature after UV shrink becomes flat within tolerance.

## Slide 32: How to Find Optimal Mold Shape?
1. Perform proposed FE analysis using mold shape reprecented by .
2. Get nodal coordinates after the analysis.
4. Apply forced displacement to the nodes of the mold.
5. Mold shape coordinates are updated to .
3. Curvature depth satisfies
?
NO
YES
Break
loop
1.
2.
3.
4.
5.
Find nodal coordinates set of the mold that minimize squared sum of curvature depth .

## Slide 33: Mold Shape Optimization (Simulation Result)
Curvature Depth Dist. on Mirror Surface
Simulation Result with Unoptimized Mold ✘ Maximum curvature depth: 1 µm
Simulation Result with Optimized Mold ✔ Maximum curvature depth: 0.01 µm
The optimized mold greatly suppressed the curvature and achieved a super-flat mirror surface!